Slide 1:
Mr. President, lady and gentlemen of the jury, I would like to thank you for the time you have dedicated to evaluating this thesis work, titled Finite Element Models for the study of hydrogen embrittlement of steel structures. This work was conducted at Mines Paris as part of a CIFRE collaboration with Transvalor and within the framework of the MESSIAH chair.
Slide 2:
- In the context of the energy transition and the decarbonization of energy sources, hydrogen plays an important role as an energy vector.
- Green hydrogen, which can be produced from renewable sources like wind and solar, offers the significant advantage of emitting no CO₂ during its production and use.
- One promising strategy to enable the use of hydrogen is to repurpose existing natural gas pipelines for hydrogen transport. In France alone, there are approximately 40,000 kilometers of pipelines, some of which are up to 80 years old, that could potentially be converted for this purpose.

Slide 3:
- However, a major challenge is that hydrogen can cause 'hydrogen embrittlement' in steels, a process that reduces their ductility and toughness and cause premature and catastrophic failure.
- In this context, the Chaire MESSIAH was created.
- In order to characterize the mechanical properties of the pipeline steels and evaluate the effect of hydrogen on it, we propose extracting small sections from the pipelines and machining mini samples to conduct experimental tests. This approach allows us to measure the material properties of the steel without service interruption.
- Explain the figures, show the specimens (tensile, fracture toughness, etc).

Slide 4:
- However, conducting experiments with sub-size specimens introduces an additional challenge regarding the transferability of results from these specimens to the full-scale structure.
- Experimental results clearly demonstrate that specimen size significantly influences toughness. As the specimen thickness increases, toughness decreases until it stabilizes at a plateau, beyond which further thickness increase has little effect.
- The figure shown here is taken from the literature and presents experimental fracture toughness values as a function of specimen thickness. This is a well-documented trend in the field, often displaying a characteristic 'bump' shape, which reflects the transition from plane stress to plane strain conditions.

Slide 5:
- Based on this context, some main objectives were defined for this thesis, which are:
  - To develop a numerical model coupling plasticity, damage and hydrogen diffusion in order to reproduce the hydrogen embrittlement phenomena, which degrades the mechanical properties of the steel, reducing its ductility, toughness and causing multi-crack initiation
- Then, to perform fracture toughness simulations using standard and sub-size specimens in order to investigate the effect of the specimen’s size and thickness on fracture toughness
- Lastly, to validate this model against experimental data from the literature and from the experiments performed during the project.

Slide 6:
Explain the topics of the presentation

Slide 7:

- When hydrogen gas molecules come into contact with the surface of the metal, they dissociate into hydrogen atoms. These atoms are then absorbed by the material and begin to diffuse throughout it.
- The solubility of hydrogen within the metal can be determined using the Sieverts' law, which states that the amount of hydrogen absorbed is proportional to the square root of the gas pressure.

Slide 8:
- The model we used for this study was initially proposed by Sofronis and later corrected by Krom. It assumes that there is a lattice hydrogen concentration (CL) which diffuses between the iron atoms and migrates toward regions of high tensile stress.
- In addition, we also consider trapped hydrogen, which represents hydrogen that gets trapped in microstructural defects. In this model, several types of traps can be simultaneously considered, and it can have a constant trap density or evolve with plastic strain.
- This model considers the Oriani’s instantaneous equilibrium between the lattice and trapped hydrogen concentrations. This means that for a isolated specimen, the total hydrogen concentration remains constant.
Slide 9:
- We applied the GTN model to simulate the material's ductile behavior. In this model, the yield surface is influenced by the total porosity, represented by the f. For a case where f=0, we retrieve the classical von Mises criterion.
- The progression of material damage is driven by two factors: void nucleation and growth. As the material deforms, these voids form and grow, contributing to the overall damage and influencing the material's mechanical response.
- The physical mechanisms of void nucleation, growth, and coalescence represented by the GTN model are based on experimentally observed phenomena, making this approach valuable for predicting material failure.

Slide 10:
- In order to simulate HE, we modified the GTN model.
- To ensure mass conservation, the void growth in the model remains unchanged.
- However, the void nucleation relation is modified to account for the effect of hydrogen.
- The added term reflects hydrogen-induced void nucleation, which weakens the cohesive bonds between atoms. This mechanism, known as hydrogen-enhanced decohesion (HEDE), contributes to increased damage and further material degradation due to the presence of hydrogen.
Slide 12:
So now we can pass to the finite element formulation of this model

Slide 13:
- The model employs a fully implicit finite strain framework and is based on a mixed formulation with four degrees of freedom: displacement (u), pressure (P), volume variation (theta), and lattice hydrogen concentration (C_L).
- The primary objective of this mixed formulation is to achieve more accurate pressure fields by avoiding volumetric locking. One key advantage of this formulation is that pressure, which is necessary for calculating the hydrogen flux, is now a degree of freedom so its gradient can be directly computed from the nodal values.
- In the figure, we can see a representation of a mesh element where only the displacement is interpolated using quadratic shape functions, while all other degrees of freedom are interpolated linearly.
- We also compare the pressure fields in the crack propagation zone of a compact tension specimen. With a standard formulation, we observe instability in the pressure fields, a case of volumetric locking. This numerical issue is effectively solved by using the mixed formulation.

Slide 14:
- Even tough the mixed formulation proved to be effective, as soon as we started to launch 3D simulation, the used of quadratic elements with additional dofs led to very high simulation times.
- Thus, another approach was used for the 3D cases:
  - The B-bar formulation employs linear elements with full integration
  - In this formulation, volumetric locking is solved by modifying the strain-displacement matrix B
  - In cases with hydrogen diffusion, to avoid extrapolating the pressure to the nodes for gradient computation, necessary for the hydrogen flux, it is also considered as a dof
- The figure contains a comparison of the mixed and the B-bar formulations and they are both effective for solving volumetric locking

Slide 15:
- A comparison of both formulations was also performed with a 3D mesh in order to compare the time needed to complete the simulations
- Both cases employed a Disk Compact Tension specimens with 5,200 elements
- The mixed formulation has more than 100,000 dofs and took 1h40 to complete
- On the other hand, the B-bar formulation has 34,000 dofs and took only 18 minutes to complete
- The Load vs. LLOD curve with both methods shows a slight difference since the linear elements are naturally stiffer since they have less nodes, but both stress fields are similar

Slide 16:
- Damage models, such as the GTN model, are known to introduce spurious mesh dependency. This means that the results can vary depending on the element size, type, and orientation used in the mesh.
- In the figures, we illustrate this mesh dependency with examples from a notched tensile specimen and a compact tension specimen. For both cases, different mesh sizes were evaluated in the crack propagation zone. The curves demonstrate that each mesh size provides different results and there is a lack of convergence, even with finer meshes.
- To address this issue, we propose using a nonlocal model based on the implicit gradient formulation.
Slide 17:
- In the nonlocal formulation, two state variables are employed: the plastic volume variation and the accumulated plastic strain. An internal length scale is associated to each of these state variables.
- We modify the damage evolution laws for void growth and nucleation by replacing these state variables with their nonlocal counterparts.
- Thus, the finite element model incorporates two additional nodal degrees of freedom: the nonlocal plastic volume variation and the nonlocal accumulated plastic strain.
- In the figure, we compare the damage field obtained using a local and a nonlocal formulation with quadratic elements. In the nonlocal model, the internal length parameter helps to smooth the regularized field.

Slide 19:
The pressurized disk tests follows a standardized method designed to assess the resistance of metallic materials to hydrogen embrittlement

The specimen used in this experiment consists on a clamped round disk with a constant thickness of 0,75 mm

The disk is subjected to a pressurization rate until its failure. The tests were carried out under hydrogen and helium in order to compare the results under both gases

However, the disk often fails in the clamping zone, making the analysis hard

This way, the first step was to redesign the disk geometry in order to control the failure location

Slide 20:

- Two new disk geometries were proposed:
  - The cup specimen is a 3 mm thickness disk with a dome machined at the center of the specimen
  - The notched specimen is a 2 mm thickness disk with a round notch
- Both geometries have the same diameter as the one proposed by the standard, this way there is no need to modify the machine setup as well as the same minimum thickness of 0,75mm as the standard geometry
- So we carried out FE simulations considering an elasto-plastic behavior in order to determine the geometry of the new specimens and here I show you a representation of it

Slide 21:

- The criterion used to determine the fracture location was the accumulated plastic strain.
- The elasto-plastic model predicts that the cup specimen tends to fail at the center, whereas the notched specimen fails at the notch.
Slide 22:

- Two steel grades were used in this study
  - A X52 vintage steel, which presents an yield strength of 400 MPa and different elongations at rupture in T and L directions
  - And a E355 modern modified steel, which presents a yield strength of 330 MPa, with higher elongation at rupture and lower ultimate tensile strength in relation to the vintage steel
- The coefficients of the elasto-plastic model were identified through optimization and a comparison between numerical and experimental results is presented here.

Slide 23:
- The simulations of the disk specimens considered an axisymmetric model employing quadratic elements with reduced integration
- The mixed formulation was employed to avoid volumetric locking
- The hydrogen diffusion coefficients were taken from the litterature
- Since damage is not considered into the numerical model, the simulations were stopped once they reached experimentally observed rupture pressure (Pr ) and the concentration and stress profiles at the rupture moment were observed
- For the hydrogen related boundary conditions, the lattice concentration is estimated from the hydrogen pressure following Sieverts’ law and is imposed to the under side of the specimen. On the upside, the lattice hydrogen is imposed zero, meaning that hydrogen can freely leave the specimen.

Slide 24:
- The curves compare the experimental and numerical results under helium for the three disk geometries in both steels. For clarity, the results for X52 steel were shifted. The curves contain the displacement at the center of the disk with respect to the gas pressure. The experiments were conducted by Luciano Santana, a fellow PhD student in the MESSIAH project.
- The results show good agreement between experimental and numerical data. The new geometries effectively controlled the fracture location, shifting it to the center for the cup disk and to the notch for the notched disk. The overlay of the fracture surface and the plastic strain field confirms that the model accurately predicts the failure location observed in the experiments.
- Failure was primarily driven by plasticity and occurred under a limit load scenario.

Slide 25:
- The curves present the experimental results under helium and hydrogen for E355 mod. steel. For simplicity, only this steel is shown, as the values for both steels are similar.
- The results indicate that hydrogen has no effect on the elasto-plastic behavior of the steel; however, the disks failed at lower pressures.
- Additionally, the rupture pressure was analyzed as a function of the pressurization rate. Surprisingly, within the range of pressurization rates considered in this study, no effect on rupture pressure was observed.

Slide 26 :
- Since the pressurization rate had no effect on rupture pressure, we investigated the embrittled thickness of the disks.
- Observations by Luciano Santana revealed that, for both steels, the hydrogen-embrittled thickness remained constant across different pressurization rates. This finding will be valuable for selecting the most appropriate trapping model.

Slide 27 :
- For simplicity, the trapping model considers only dislocations as traps.
- The trap binding energies and trap densities were taken from the literature.
- In the literature, two main values for the trap binding energy are commonly used: 40 and 60 kJ/mol.
- For trap densities, two exponential functions increasing with accumulated plastic strain were analyzed. Both functions start at similar values at zero strain; however, the model proposed by Moro et al. increases rapidly, saturating at a high trap density even at low strain levels.
- These different coefficients and relationships will be used in the upcoming simulations, and the results will be compared with experimental observations.

Slide 28 :
- Four models were derived from the binding energy and trap density values found in the literature.
- These models were tested on the three specimens, and the results for the notched specimen are presented here for two pressurization rates.
- The simulations using the model from Moro show different penetration profiles for the two pressurization rates, which contradicts the experimental observations where the embrittled depth remains constant across different rates.
- In contrast, the model proposed by Sofronis produces similar penetration profiles at different rates. Since this model considers only dislocations as traps, which have relatively low binding energies, a binding energy value of 40 kJ/mol was chosen for the next simulations.

Slide 29:
- The final analysis of this test examined the relationship between principal stress and hydrogen pressure.
- The curve shows the evolution of principal stress as a function of hydrogen pressure for both steels across the three disk specimens.
- The principal stress was determined by analyzing the maximum value at integration points within the rupture zone.
- Specimens with geometries that develop higher principal stress in the fracture zone fail at lower Pa​ (H2​).
- Further analysis was conducted to investigate the correlation between principal stress and hydrogen concentration in the fracture zone. Two pressurization rates were tested for each of the three geometries, for both steels. The results show that as hydrogen concentration increases in the fracture zone, the critical principal stress required to initiate fracture decreases.

Slide 31:
- The database used in this study was published by a French research group from CEA, who explored the impact of gaseous hydrogen on the mechanical properties of steel.
- The material analyzed is a high-strength steel exposed to both hydrogen and a neutral gas environment.
- The coefficients used in our model were taken from the literature.
- Given that hydrogen embrittlement is associated with quasi-cleavage behavior, we introduced a stress-dependent factor into the nucleation law. Specifically, when the principal stress σI exceeds a critical threshold, we assume a constant nucleation rate, leading to increased damage.
- With this model, hydrogen exponentially decreases the critical stress to trigger void nucleation

Slide 32:
- We conducted tensile tests on axisymmetric specimens under various strain rates, with the surface of the specimens exposed to hydrogen.
- The experimental results revealed that hydrogen presence led to crack initiation on the surface of the specimens.
- The strain rate had a pronounced effect on the test results. In the slowest tests, hydrogen had sufficient time to diffuse all the way to the center of the specimen. As a result, failure occurred at the center, followed by a significant ductility loss.
- For a certain range of intermediate strain rates, surface fractures were observed, though the ductility loss was less pronounced than in the slowest tests. Finally, at higher strain rates, hydrogen diffusion was limited, and a classical ductile failure occurred with only a minor reduction in ductility. This demonstrates the important relationship between strain rate and hydrogen's influence on material behavior.

Slide 33:
- We also compared the damage evolution at the center and the surface of the specimen under air and hydrogen conditions. Please note that the y-axis is in logarithmic scale. We can observe very distinct behaviors between the two environments.
- In the hydrogen environment, the video shows the formation of multiple surface cracks, with one dominant crack propagating further than the others.

Slide 34:
- We conducted again the pressurized disk tests, but this time using only the geometry proposed by the standard, with constant thickness, based on the experimental data from Moro et al.
- The plot shows the displacement at the center of the disk as a function of gas pressure. The test conducted under hydrogen demonstrates a lower failure pressure, indicating a reduction in ductility compared to tests conducted under other conditions.
- Additionally, the plot reveals a gradient in the lattice hydrogen concentration field. This gradient results from the boundary conditions imposed during the test. The trapped hydrogen concentration is notably higher in the region where plastic strain is at its maximum, further illustrating the impact of hydrogen on material behavior and failure mechanisms.

Slide 35:
- Similar to the analysis performed on the tensile tests, we also investigated the effect of pressurization rate in the disk tests. The plot presented here shows failure pressure as a function of pressurization rate for both experimental and numerical data under hydrogen and helium.
- Despite significant scatter in the experimental data, the numerical results reveal a clear trend. Specifically, under hydrogen, a lower pressurization rate is associated with increased susceptibility to hydrogen embrittlement. This is due to the longer time available for hydrogen to diffuse into the material, increasing its embrittlement.
- Additionally, we observe the total hydrogen concentration inside the specimen for both the slowest and fastest test. The data confirms that the slowest test has a higher hydrogen concentration, consistent with the observed effects of slower pressurization rates.
- The tests conducted by Luciano did not show any effect of the pressurization rate at the analyzed rates. The results from Briottet show that at the same range of pressurization rates, the failure pressure is constant and that it increases only at higher pressurization rates.

Slide 36:
- The final test we conducted was the fracture toughness test with a compact tension specimen, imposing an uniaxial displacement in environments of both air and hydrogen at a pressure of 30 MPa.
- In this test, when an element within the material reached a maximum critical porosity it is considered broken and the corresponding lattice concentration was imposed to the newly formed crack.

Slide 37:
- In our analysis, we determined the crack length through post-processing, which involved identifying and evaluating the broken elements. The J-integral was computed using standard methods to assess the material's fracture toughness.
- The presented curve compares the results obtained under air and hydrogen environments. Notably, there is a significant decrease in the J-integral values for tests conducted under hydrogen, indicating reduced fracture toughness in the presence of hydrogen.
- Additionally, we observed the evolution of the total hydrogen concentration inside the specimen. The concentration increased over time and as the crack propagated.

Slide 39:
- The last analysis concerned the standard and sub-size compact tensions specimens. Only the results of the X52 steel, which was provided in the form of a tube with 7,92mm thickness, are presented here. All the simulations were carried out without hydrogen.
- The figure contains a representation of the specimens, which were pre-cracked and presented side grooves on both sides.
- The macro specimen had a thickness of 7.5 mm, while the sub-size specimens had thicknesses of 2 mm and 5 mm.

Slide 40:
- The numerical model utilized linear elements with full integration and the B-bar formulation to mitigate volumetric locking.
- Damage was captured using a nonlocal GTN model with two internal length scales: one linked to the accumulated plastic strain for void nucleation and the other to plastic volume change for void growth.
- While a typical element size in nonlocal models for pipeline steels is 100 µm, the internal length associated with void nucleation was set to 33 µm.
- To ensure consistency with the internal length scale, the mesh elements in the crack propagation zone were sized accordingly: their height was set to one-third of the internal length, while their length was approximately twice their height.

Slide 41:
- During the simulation, when a predefined number of integration points in an element reached the critical porosity value fc​, the element was removed, leading to material softening observed during crack propagation.
- Two methods were used to compute crack propagation:
- The first method relied on the compliance technique, where crack advance was determined in the same manner as in the experiments.
- While straightforward, this approach has the drawback of significantly increasing simulation time, as it requires incorporating loading, holding, and unloading steps.
- The figure illustrates crack propagation during the simulation and compares the load vs. LLOD curves between the experiment and the compliance-based simulation.

Slide 42 :
- The second method was based on post-processing.
- First, the initial crack front was identified, and porosity values were analyzed in elements within the crack propagation zone.
- Next, elements containing integration points that reached the critical porosity value were considered broken, the crack front was updated, and crack propagation was computed.
- The figure compares the two crack propagation techniques. Since both methods yield nearly identical results, but the post-processing approach is significantly faster, it will be used for future simulations.

Slide 43 :
- The coefficients of the constitutive law were identified directly from fracture toughness specimens through an optimization process.
- The hardening law used here differs slightly from that in the disk simulations due to material dispersion.
- The following elasto-plastic and damage coefficients will be used in the next simulations.

Slide 44 :
- The curves compare the load vs. LLOD responses between experimental and numerical results for the three specimen sizes.
- The mesh dimensions matched those of the tested specimens.
- While the elasto-plastic model fails to accurately represent the fracture toughness test once crack propagation begins, the overall experimental behavior was well captured by the numerical model.

Slide 45:
- This figure compares experimental and numerical results for the J vs. da and CTOD vs. da curves across the three specimen sizes. The J-integral values were computed following ASTM standards.
- The X52 steel exhibits relatively low toughness.
- In the simulations, crack propagation initiates later than in the experiments. This delay was partially addressed by reducing the void nucleation threshold, but beyond a certain point, it no longer influenced the results.
- For both the J and CTOD curves, toughness increases as specimen size decreases.

Slide 46:
- The detailed view highlights a comparison of the J-da curves between experiments and simulations. A comparison of J0.2​ and J0.5​ values is also provided.
- The construction line was obtained following ASTM standards.
- According to the standard, the entire test is valid for the mDCT-5 and CT-7.5 specimens.
- Overall, good agreement is observed for the mDCT-2 and mDCT-5 specimens. However, the delay in crack propagation onset for the macro specimen could not be fully addressed.

Slide 47:
- The same analysis was conducted for the CTOD-da curves.
- The CTOD results show a slightly better fit to the experimental data, but the overall behavior remains consistent.

Slide 48:
- We now focus on the effect of specimen size on fracture toughness.
- To investigate this, we analyzed six homothetic compact tension specimens, systematically scaling their dimensions from the smallest to the largest.
- For all specimens, the ratios B/W and a0​/W were kept constant at 0.5 and 0.55, respectively.
- Each mesh was individually generated to ensure proper element sizing relative to the internal length.
- Please note that the two smallest specimens are impractical to machine due to their reduced size.

Slide 49:
- Next, the second analysis examined the effect of thickness on fracture toughness.
- A CT-12.5 specimen was used as a reference, and its thickness was systematically varied.
- Unlike the previous case, all specimens in this study can be machined.

Slide 50:
- The first set of results used the constitutive law coefficients identified for X52 steel.
- The results indicate that homothetic specimens have a minor effect on fracture toughness.
- However, for the varying thickness specimens, toughness decreased as thickness increased in this configuration.

Slide 51 :
- We plotted the J0.2​ and J0.5​ values against specimen thickness for both the homothetic and varying thickness specimens.
- For the homothetic specimens, the results remain relatively stable, whereas for the varying thickness specimens, fracture toughness strongly depends on thickness.
- Specifically, the J0.5​ curve exhibits a half-bump shape, similar to the trend observed in the literature and presented in the introduction.
- Additionally, we observe that fracture toughness does not follow a bijective relationship, meaning different specimens with the same thickness do not necessarily exhibit the same toughness value.

Slide 52 :
- Lastly, to explore the effect of ductility on fracture toughness, we maintained the hardening fit for X52 steel while modifying the GTN coefficients q1 and q2.
- Increasing q1 enhances void growth sensitivity, leading to earlier void growth and reduced ductility.
- Increasing q2 accelerates crack initiation, also reducing ductility.
- In all cases, low void nucleation values were used, with nucleation occurring at high plastic strain levels, ensuring that void nucleation had a minimal effect on this analysis.

Slide 53 :
- The results show that the homothetic specimens exhibit more stable fracture toughness values, while the varying thickness specimens display the characteristic "bump shape."
- More ductile materials appear to be more sensitive to size effects.
- The Jmax​ values were computed according to ASTM standards, and all points to the right of this line are considered valid. However, even tests classified as valid exhibit sensitivity to specimen size.
- Once again, no bijective relationship can be established between fracture toughness and thickness.