Slide 1:
- Thank the presenter, the jury and the people present
- Introduce the thesis title and the context (Mines Paris, CIFRE avec Transvalor, chaire MESSIAH)

Slide 2:
- In the context of the energy transition and the decarbonization of energy sources, hydrogen plays an important role as an energy vector.
- Green hydrogen, which can be produced from renewable sources like wind and solar, offers the significant advantage of emitting no CO₂ during its production and use.
- One promising strategy to enable the use of hydrogen is to repurpose existing natural gas pipelines for hydrogen transport. In France alone, there are approximately 40,000 kilometers of pipelines, some of which are up to 80 years old, that could potentially be converted for this purpose.

Slide 3:
- However, a major challenge is that hydrogen can cause 'hydrogen embrittlement' in steels, a process that reduces their ductility and toughness and cause premature and catastrophic failure.
- In this context, the Chaire MESSIAH was created.
- In order to characterize the mechanical properties of the pipeline steels and evaluate the effect of hydrogen on it, we propose extracting small sections from the pipelines and machining mini samples to conduct experimental tests. This approach allows us to measure the material properties of the steel without service interruption.
- Explain the figures, show the specimens (tensile, fracture toughness, etc).

Slide 4:
- Experimental results clearly demonstrate that specimen size significantly influences toughness. As the specimen thickness increases, toughness decreases until it stabilizes at a plateau, beyond which further thickness increase has little effect.
- The figure shown here is taken from the literature and presents experimental fracture toughness values as a function of specimen thickness. This is a well-documented trend in the field, often displaying a characteristic 'bump' shape, which reflects the transition from plane stress to plane strain conditions.

Slide 5:
- Based on this context, some main objectives were defined for this thesis, which are:
  - To develop a numerical model coupling plasticity, damage and hydrogen diffusion in order to reproduce the hydrogen embrittlement phenomena, which degrades the mechanical properties of the steel, reducing its ductility, toughness and causing multi-crack initiation
- Then, to perform fracture toughness simulations using standard and sub-size specimens in order to investigate the effect of the specimen’s size and thickness on fracture toughness
- Lastly, yo validate this model against experimental data from the literature and from the experiments performed during the project.

Slide 6:
Explain the topics of the presentation

Slide 7:

- When hydrogen gas molecules come into contact with the surface of the metal, they dissociate into hydrogen atoms. These atoms are then absorbed by the material and begin to diffuse throughout it.
- The solubility of hydrogen within the metal can be determined using the Sieverts' law, which states that the amount of hydrogen absorbed is proportional to the square root of the gas pressure.

Slide 8:
- The model we used for this study was initially proposed by Sofronis and later corrected by Krom. It assumes that there is a lattice hydrogen concentration (CL) which diffuses between the iron atoms and migrates toward regions of high tensile stress.
- In addition to free hydrogen, we also consider trapped hydrogen, which represents hydrogen that gets trapped in microstructural defects. In this model, several types of traps can be simultaneously considered, and it can have a constant trap density or evolve with plastic strain.
- A key assumption of this model is that there is an equilibrium between the free and trapped hydrogen concentrations. This means that for a isolated specimen, the total hydrogen concentration remains constant.
Slide 9:
- We applied the GTN model to simulate the material's ductile behavior. In this model, the yield surface is influenced by the total porosity, represented by the f. For a case where f=0, we retrieve the classical von Mises criterion.
- The progression of material damage is driven by two factors: void nucleation and growth. As the material deforms, these voids form and grow, contributing to the overall damage and influencing the material's mechanical response.
- The physical mechanisms of void nucleation, growth, and coalescence represented by the GTN model are based on experimentally observed phenomena, making this approach valuable for predicting material failure.

Slide 10:
- In order to simulate HE, we modified the GTN model.
- To ensure mass conservation, the void growth in the model remains unchanged.
- However, the void nucleation relation is modified to account for the effect of hydrogen.
- The added term reflects hydrogen-induced void nucleation, which weakens the cohesive bonds between atoms. This mechanism, known as hydrogen-enhanced decohesion (HEDE), contributes to increased porosity and further material degradation due to the presence of hydrogen.

Slide 12:
So now we can pass to the finite element formulation of this model

Slide 13:
- The model employs a fully implicit finite strain framework and is based on a mixed formulation with four degrees of freedom: displacement (u), pressure (P), volume variation (theta), and lattice hydrogen concentration (C_L).
- The primary objective of this mixed formulation is to achieve more accurate pressure fields by avoiding volumetric locking. One key advantage of this formulation is that pressure, which is necessary for calculating the hydrogen flux, is now a degree of freedom so its gradient can be directly computed from the nodal values.
- In the figure, we can see a representation of a mesh element where only the displacement is interpolated using quadratic shape functions, while all other degrees of freedom are interpolated linearly.
- We also compare the pressure fields in the crack propagation zone of a compact tension specimen. With a standard formulation, we observe instability in the pressure fields, a case of volumetric locking. This numerical issue is effectively solved by using the mixed formulation.

Slide 14:
- Even tough the mixed formulation proved to be effective, as soon as we started to launch 3D simulation, the used of quadratic elements with additional dofs led to very high simulation times.
- Thus, another approach was used for the 3D cases:
  - The B-bar formulation employs linear elements with full integration
  - In this formulation, volumetric locking is solved by modifying the strain-displacement matrix B
  - In cases with hydrogen diffusion, to avoid extrapolating the pressure to the nodes for gradient computation, necessary for the hydrogen flux, it is also considered as a dof
- The figure contains a comparison of the mixed and the B-bar formulations and they are both effective for solving volumetric locking

Slide 15:
- A comparison of both formulations was also performed with a 3D mesh in order to compare the time needed to complete the simulations
- Both cases employed a Disk Compact Tension specimens with 5,200 elements
- The mixed formulation has more than 100,000 dofs and took 1h40 to complete
- On the other hand, the B-bar formulation has 34,000 dofs and took only 18 minutes to complete
- The Load vs. LLOD curve with both methods shows a slight difference since the linear elements are naturally stiffer since they have less nodes, but both stress fields are similar